PRODUCT SPECIFICATION CSI FORMAT

Slope and Channel Grid Systems

February 2018

Cell-Tek Geosynthetics LLC

809 Barkwood Court, Suite M

Linthicum Heights, MD 21090

USA

Toll Free (888) 851-0051

Phone (410) 721-4844

Fax (410) 721-3844

E-Mail info@celltekdirect.com

Website www.celltekdirect.com

This specification utilizes the Construction Specifications Institute (CSI) Format, including MasterFormat (2004 Edition), SectionFormat, and PageFormat, contained in the CSI Manual of Practice.  Optional text is indicated by brackets [ ], delete optional text in your final copy.  Delete Specifier Notes which precede some sections.  Each section must be carefully reviewed by the Engineer

to meet the requirements of the project and local building code.

SECTION 02340

SOIL STABILIZATION SYSTEM

Specifier Notes: This section covers Cell-Tek Geosynthetics Slope Grids (geocell) Cellular Confinement Systems. The systems are comprised of the following basic components:  Slope Grid (geocell), one or more infill materials, a geotextile fabric, earth anchoring devices, tendons, u-bolts, geogrids, geomembranes, geocomposite drainage materials, and possibly surface treatments.

PART 1 GENERAL

Specifier Note:  Revise any part of the sections below to suit project requirements.

1.01 SUMMARY

A. Cellular confinement system utilized for slope protection.

1.02 RELATED SECTIONS

A. Section 02250 - Shoring and Under Pinning

B. Section 02260 - Excavation and Protection

C. Section 02300 - Earthwork

D. Section 02330 - Embankment

E. Section 02370 - Erosion and Sedimentation Control

F. Section 02390 - Shoreline Protection and Mooring Structure

1.03 REFERENCES

A. AASHTO M 218 - Steel Sheet, Zinc-Coated (Galvanized) for Corrugated Steel Pipe

B. AASHTO M 288 - Geotextile Specification for Highway Applications

C. ASTM D 1505 - Density of Plastics by the Density-Gradient Technique

D. ASTM D 1693 - Environmental Stress-Cracking of Ethylene Plastics

E. ASTM D 5199 - Measuring Nominal Thickness of Geotextiles and Geomembranes

F. ASTM E 41 - Terminology Relating to Conditioning

1.04 SYSTEM DESCRIPTION

Specifier Note: Edit the following as required for the project.

A. Cellular confinement system involves a three-dimensional geocell material into which specific infill   materials are placed. It is composed of a set of virgin polyethylene strips which are ultrasonically welded together at certain intervals, creating seams aligned perpendicular to longitudinal axis of strips.  When expanded, this structure creates a flexible, three-dimensional matrix of connecting cells.

B. Complete slope protection systems includes Slope Grid sections, cell infill materials and some or all of the following items:  [geotextiles], [geogrids], [geomembranes], [geocomposite drainage materials], [tendons], [stake anchors], [u-bolts], and [surface treatments].

1.05 SUBMITTALS

A. Product Data: Submit product data provided by manufacturer.

B. Technical Drawings: Submit manufacturer's technical drawings including section layout, direction of

expansion, tendon locations, u-bolts and anchor stake locations.

C. Samples: Submit manufacturer's samples.

1. Geocell sections

2. Tendons

3. Geotextile swatch

4. Stake anchors

5. U-bolts

6. Any geosynthetic components, if required

7. [Specimen of infill materials, if required]

D. Material Certification: Submit certifications of the polyethylene material used to make geocell

material.

1. Certification of percentage of carbon black provided by manufacturer

2. Certification of polyethylene density (ASTM D1505) and ESCR (ASTM D1693) provided by     manufacturer

1.06 QUALITY ASSURANCE

A. Manufacturer's Qualifications: Quality management system certified to ISO 9001:2000.

B. Installation:  Choose an installer with a satisfactory record of performance on projects of comparable   size, complexity, and quality.

1.07 DELIVERY, STORAGE, AND HANDLING

A. Delivery: Deliver materials in manufacturer's original packaging with identification labels clearly   intact.

B. Storage:

1. Store materials per manufacturer's instructions.

2. Store materials out of direct sunlight.

C. Handling: Use care when unwrapping, handling, expanding, and infilling grid sections.

1.  Be certain to overfill cells prior to any load bearing or vehicular traffic.

PART 2 PRODUCTS

2.01 MANUFACTURER

A. Cell-Tek Geosynthetics LLC, 809 Barkwood Court, Suite M, Linthicum Heights, MD 21090

Toll Free (888) 851-0051. Phone (410) 721-4844. Fax (410) 721-3844.

E-Mail info@celltekdirect.com. Website www.celltekdirect.com.

2.02 Cell-Tek Slope Grid CELLULAR CONFINEMENT SYSTEM

Specifier Note: All measurements are subject to manufacturing tolerances, unless otherwise

specified.

A. Base Materials:

1. Virgin Polyethylene Stabilized with carbon black:

a. Density, ASTM D 1505: 0.9574 g/cm3 (59.77 pounds per cubic foot)

b. Environmental Stress Crack Resistance (ESCR), ASTM D 1693: 3,500 hours

c. Ultra-Violet Light Stabilization: Certified 1.55% carbon black, homogeneously distributed throughout material

B. Strip Properties:

1. Perforated and Textured Strip/Cell:

a. Strip Sheet Thickness, ASTM D 5199: 1.42 mm, minus 5 percent, plus

10 percent

b. Polyethylene Strips: Textured surface with a multitude of rhomboidal (diamond

shape) indentations

c. Polyethylene Strips: Perforated with horizontal rows of 9.5 mm (0.37 inch) diameter

holes

d. Perforations Within Each Row: 20 mm (0.79 inch) on-center

e. Horizontal Rows: Staggered and separated 13 mm (0.51 inch) relative to hole

centers

f. Edge of Strip to Nearest Edge of Perforation: 7.4 mm (0.29 inch) minimum

g. Centerline of Spot Weld to Nearest Edge of Perforation: [45.45 mm (1.79 inches) minimum]

2.  Weld Spacing:

a. Weld Spacing for [Slope Grid Sections: 432 mm plus or minus 2.5 mm (17.0 inches

plus or minus 0.10 inch)]

C. Cell Properties:

1. Individual Cells: Uniform in shape and size when expanded.

Specifier Notes: Specify either Slope Grid, SLP400™ or Slope Grid, SLP600™.  Consult Cell-Tek Geosynthetics, LLC for suitable product type and cell size.

2. Individual Cell Dimensions: SLP400™-Cell Detail

Nominal Dimensions ± 10%

a. Length 315 mm (12.4 inches)

b. Width 271 mm (10.7 inches)

c. Nominal Area plus or minus 1%: 427 cm2 (66 square inches)

d. Nominal Depth: 100 mm (4 inches).

4. Individual Cell Dimensions: SLP600™-Cell Detail

Nominal Dimensions ± 10%

a. Length 315 mm (12.4 inches)

b. Width 271 mm (10.7 inches)

c. Nominal Area plus or minus 1%: 427 cm2 (66 square inches)

d. Nominal Depth: 150 mm (6 inches).

D. Cell Seam Strength Tests:

1. Short-Term Seam Peel-Strength Test:

a. Cell Seam Strength: Uniform over full depth of cell.

b. Minimum Seam Peel Strength: 1542 N  (347 lbf) for 100 mm (4 inch) depth, 2170 N (488 lbf) for 150 mm (6 inch) depth

2. Long-Term Seam Peel-Strength Test:

a. Conditions: Minimum 7 days in a temperature-controlled environmental chamber that

undergoes fluctuation on a 1-hour cycle from room temperature (per ASTM E 41) to 54   degrees C (130 degrees F)

b. Testing is conducted on the seam of 100 mm (4 inch) cell depth specimens.

c.  Test Method:  Seam shall support a 72.5 kg (160 pound) load for a minimum of 7  days.

E. Section Types and Sizes:

Specifier Note:  Consult Cell-Tek Geosynthetics for assistance in specifying appropriate product type and cell depth.

1. Cell Size: 100 mm (4") - SLP400™

a.  Section Length: 8.7 m (29 feet)

b.  Section Width: 2.4 m (8 feet)

c.  Section Area: 20.88 square meters (232 square feet)

3.  Cell Size: 150 mm (6") - SLP600™

a.  Section Length: 8.7 m (29 feet)

b.  Section Width: 2.4 m (8 feet)

c.  Section Area: 20.88 square meters (232 square feet)

2.03 TENDON REQUIREMENTS

Specifier Notes: Specify tendons required to meet design requirements by tendon style for the application. Consult Cell-Tek Geosynthetics for assistance.

A. Tendon Style:

1. [GAC-A] [GAC-B]*

*Specifier Note:  If engineer has specified break strength other than what is listed please          consult Cell-Tek Geosynthetics for the proper tendon style.

a. Material: Galvanized high carbon steel aircraft cabling, type 6, small cords

b. GAC-A (3/16” diameter with 3,700 break strength, GAC-B (1/4” diameter with 6,100 break strength).

2.04 ANCHORING COMPONENTS

Specifier Notes: Specify required anchoring components and delete the others. Choose from

options for galvanizing and rod diameter for the steel stakes. Provide data for the wood stakes.

Consult Cell-Tek Geosynthetics for assistance.

A. Steel J-Pin Stakes:

1. Material: Mild steel or reinforced steel rod

2. [Galvanizing: AASHTO M 218]

3. Return: Minimum-radius, 180-degree return at one end

4. Rod Diameter: [10 mm (0.375 inch)] [13 mm (0.50 inch)] [16 mm (0.625 inch)] [19 mm   (0.75 inch)]

5. Stake Length: As indicated on the drawings

B. Straight Steel Stakes:

1. Material: Mild steel or reinforcing steel rod

2. [Galvanizing: AASHTO M 218]

3. Rod Diameter: [10 mm (0.375 inch)] [13 mm (0.50 inch)] [16 mm (0.625 inch)] [19 mm  (0.75 inch)]

4. Stake Length: As indicated on the drawings

C. Wood Stakes:

1. Wood Type: ____________________ , free of knots that may diminish strength

2. Cross Section: _______________ by _______________

3. Length: _______________

2.05 U-BOLTS

Specifier Notes:  Specify required anchoring components and delete the others.

Consult Cell-Tek Geosynthetics for assistance.

- U-Bolt Style:

1. [U-Bolt-A] [U-Bolt-B]

a. Material: Cast malleable iron wire rope clip, drop forged galvanized wire rope clip / forged carbon steel

b. GAC-A (for use with 3/16” tendon, GAC-B (for use with 1/4” tendon).

2.06 RELATED GEOSYNTHETIC COMPONENTS

Specifier Notes: Specify related geosynthetic components required for the application. Consult

Cell-Tek Geosynthetics for assistance in determining requirements.

A. Geotextiles: AASHTO M 288

B. Geocomposite Drainage Materials:

C. Geogrid and Geotextile Sheet Reinforcement:

D. Geomembrane and Impervious Barriers:

2.07 CELL INFILL MATERIALS

Specifier Notes: Specify cell infill materials based on nature and size of design loads. Specify

combinations of infill types to meet required range of performance requirements. Consult Cell-Tek Geosynthetics LLC for assistance in determining requirements.

A. Cell infill materials include one or a combination of the following:

1. Sand

2. Gravel and crushed rock or stone with a maximum particle size of 75 mm (3 inches) for

erosion control applications

3. Concrete and soil-cement mixes

4. For slope surface stabilization and erosion control applications, infill with screened topsoil,

free of foreign material.

2.07 SURFACE TREATMENTS

Specifier Notes: Specify surface treatments of infilled geocell system.

A. Surface treatment includes one or a combination of the following:

1. Vegetation

2. Degradable revegetative blankets

3. Turf reinforcement mats

4. Sprayed emulsions and binders

5. Aggregates

PART 3 EXECUTION

3.01 EXAMINATION

A. Evaluate site conditions. Notify the Engineer and refrain from excavation until site conditions have

been corrected.

B. Evaluate the layout of the project as indicated on the drawings. Notify the Engineer and do not

proceed until the layout of the project matches the drawings.

Specifier Notes: Edit the installation requirements as required for the project. Consult Cell-Tek Geosynthetics for assistance in determining requirements.

3.02 INSTALLATION OF SLOPE PROTECTION SYSTEMS

A. Prepare subgrade and install according to manufacturer's instructions.

B. Subgrade Preparation:

1. Excavate and shape foundation soils in order for installed Slope Grid sections to be flush with or slightly lower than surrounding terrain or final grade as indicated on the drawings or as directed by the Engineer.

2. Install non-woven geotextile underlayer, if specified, confirming required overlaps are     maintained and outer edges of geotextile are buried a minimum of 150 mm (6 inches) below grade.

C. Positioning and Anchoring without Tendons:

1. Anchor Slope Grid sections at crest of slope. Use type of anchor and frequency of anchoring as indicated on the drawings or as directed by the Engineer.

2. Expand Slope Grid sections down slope. Confirm each section is expanded

uniformly to required dimensions and outer cells of each layer are correctly aligned.

Interleaf or overlap edges of adjacent sections in each layer, joining the grid sections per manufacturer's installation instructions to create a continuous matrix of cells. Confirm upper surfaces of adjoining sections are flush at joint and adjoining cells are fully anchored. Anchor with specified anchors in a prescribed pattern throughout slope surface.

D. Placement and Anchoring with Tendons:

1. Feed precut lengths of tendon material through holes in cell walls of Slope Grid section before expanding individual sections into position. Secure tendons so that tendons remain in place while sections are being expanded.

2. Anchor tendons and Slope Grid sections at the crest of the slope and expand down slope.

3. In cases where penetration of subgrade is allowed, anchor tendons and Slope Grid with specified anchors in prescribed pattern throughout slope surface.

E. Placement of Infill:

1. Put specified infill materials into expanded cells with suitable material handling equipment,    such as a backhoe, front-end loader, conveyor, or crane-mounted skip. Drop height must not exceed 1 m (3 feet). Avoid displacement of Slope Grid sections by infilling from crest to bottom of slope. Overfill and compact infill according to the consistency of material and cell depth as follows:

a. Overfill screened topsoil between 25 to 50 mm (1 to 2 inches) and lightly tamp or roll

so that soil is even with top edge of cell walls. Apply specified surface treatment.

b. Overfill loose granular materials approximately 25 mm (1 inch) and compact with a

plate tamper or backhoe bucket. Remove loose surface material so infill is even with

top edges of cells.